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EVERBUILD MULTI-PURPOSE WOOD FILLER AND STOPPER is an easy to use ready mixed premium joiners grade filler ideal for filling small imperfections (max 5mm depth) in wood. Once dry, the filler leaves a sandable surface, which can be stained, painted, varnished or dyed, even with microporous stains. The filler is waterproof when dry and hence is suitable for exterior as well as interior applications. 


· Non hazardous water based filler
· Non flammable
· Low odour
· Ready to use – no mixing of components required.

· Filling small holes, splits, surface imperfections and damaged areas in wood.

· Covering the recesses left by nails and screws.

 
· As the filler may absorb some stains at different rates to the surrounding timber, always test a small area first. Note: filler may dry darker.

· Do not exceed 5mm in one coat. For holes deeper than 5mm or for areas subject to impact such as doors and window frames, use EVERBUILD HIGH PERFORMANCE WOOD FILLER which can be applied to any depth and is shatterproof.
· Protect from rain when used externally for at least 5 hours.
· Do not apply below 5`C.
· As the manufacturer cannot know all the uses its products may be put to, it is the users responsibility to determine suitability for use. If in doubt, contact technical services department for advice.

NOTE: If you intend to overstain the wood once filled ALWAYS CHOOSE THE COLOUR OF FILLER THAT NEAREST MATCHES THE WOOD YOU ARE FILLING NOT THE STAIN YOU INTEND TO USE. THIS FILLER MAY DRY TO A SLIGHTLY DARKER SHADE.

As the filler may absorb some stains at different rates to the surrounding timber, always test a small area first.

Before applying, ensure surfaces are clean, dry, sound and free from dust or any contaminants which 

may affect adhesion

.. 
Stir well before use and apply with a spreader or knife. Fill the hole proud to allow for sanding. Once dry, sand to a smooth finish and apply required stain. 



BASE





Styrene Acrylic copolymer









CONSISTENCY




Stable paste


SPRCIFIC GRAVITY



ca. 1.8


TOUCH DRY




15 minutes @ 20`C


THROUGH HARD



2 hours @ 20`C


SANDABLE




30 minutes @ 20`C


OVERPAINTABLE



2 Hours @ 20`C


APPLICATION TEMPS



+5oC to +40oC. (Optimum 20oC).


TEMPERATURE RESISTANCE


-5oC to +70oC. 



. 
Consult MSDS for full list of hazards.

Store in cool dry conditions, away from direct sunlight between 10 and 20oC . PROTECT FROM FROST.


12 months in original containers at stated storage temperatures.

                                 EVERBUILD MULTI-PURPOSE WOOD FILLER
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